| TAUBER OIL COMPANY (TYPICAL) MARINE GASOIL ANALYSIS |
| --- |
| TEST | METHOD | RESULT | UNITS |
| Lubricity | D-6079 | 457 | um |
| Viscosity, cSt @ 104°F | D-445 | 3.055 |  |
| API | D-4052 | 33.4 |  |
| Cetane Index | D-979 | 46 |  |
| Flash Point, PMCC °F | D-93 | 152 |  |
| Pour Point | D-97 | -18 | °C |
| Ash | D-482 | <0.001 | Wt.% |
| Hydrogen Sulfide Content | IP 570 | < 2 | Ppm |
| Sulfur | D-2622 | 9 | ppm |
| These specifications are typical and subject to change. |

# Text boxes

12/30/14